731464.006.

8 ребер = 8 ribs

2 фаски = 2 chamfers

2 бобышки = 2 bosses

2 отв. = 2 holes

3 места = 3 places

- The substitution of the material AK9M2 in accor. to standard GOST 1583-93 is permitted.

- Casting precision 5-0-0-7 GOST 26645-85.

- Unspecified pattern tapers max. 2o.

- Unspecified pattern radii max. 2 mm.

- The base surfaces must be clean, without scar and burr.

- Burr on the surfaces Ч, Ш, Щ, Э, Ю, Я is not allowed.

- Pressure die casting, porosity class max. 3.

- Surface condition per reference sample.

- The workpiece is to shot blast, the surface condition per reference sample.

- Nonuniform areas on the shot blast surface, scratches are not allowed.

- The order number of the press mold and the nest number are to mark in font 3-Pr3 convex 0,5…0,8 mm in accor. to standard STB 992-95.

- The design letters “SR 16033” are to mark in font 3-Pr3 convex 0,5…0,8 mm in accor. to standard STB 26.008-85.

- * Dimensions are to implement by tool.

- General tolerances in accor. to standard GOST 30 893.2 – mK.

- On the processed surfaces, except surfaces A, Б and B, single holes with the largest value of 1 mm, not remediated, in quantity 2 holes on a separate surface, but  not more than 6 on the whole component are allowed.

- Rest technical requirements according to standard STB 1014-95.